RP Schmitz
This paper was written for and presented at the 17th Analysis and Computation Specialty Conference held in conjunction with the 2006 ASCE Structures Congress held in St. Louis, MO

ABSTRACT

## INTRODUCTION
BACKGROUND
Concrete International

Array
Array
Proposed Design Procedure

## ANALYSIS METHODOLOGY AND MATERIALS
Finite Element Analysis (FEA) Model Development
The Fabric Model and Material Properties
- R
Material Properties of Geotextile Fabrics

Array
Array
TABLE 1	AMOCO 2006 GEOTEXTILE FABRIC MATERIAL PROPERTIES
t = 0.03-in	Fabric thickness
Ewarp = Ea = 46,667 psi	Modulus of Elasticity, Machine Direction
Efill = Eb = 90,000 psi	Modulus of Elasticity, Cross Machine Direction
G = 23,333 psi	Shear Modulus
v = 0.0	Poisson's Ratio

Relaxation and Creep in Geotextile Fabrics
ANIMATIONS
ADINA Fabric Model
ba
aaa…………………
bbb…

a
b
a
b
The Slurry Model and Material Properties
TABLE 2	SLURRY MATERIAL PROPERTIES
t = varies-in	Slurry thickness
E = 2 psi	Modulus of Elasticity
vsm = 0.0	Poisson's Ratio
wtsm = 145 lbs/ft3	Weight
Dsm = 0.00021716366 lb-sec2/in4	Density

## PANEL DESIGN AND OPTIMIZATION
Step 1 – Determination of Load Paths
Array
Array
Array
Step 2 – Define Fabric Formwork Design
“B”
Step 3 – “Form finding” the Panel Shape
ANIMATIONS
Step 4 – Panel Analysis and Design
Array
Array
Array
Array
uDc………………………
uW………
c
uD
uW
TABLE 4	CONCRETE MATERIAL PROPERTIES		TABLE 5	REINFORCING MATERIAL PROPERTIES
t = varies-in	Concrete panel thickness		Es = 29,000,000 psi	Young's Modulus of Elasticity
Ec = 4,074,281 psi	Secant Modulus of Elasticity		Ets = 290,000 psi	Strain hardening (Tangent) Modulus
Etc = 7,129,991 psi	Initial Tangent Modulus of Elasticity (Assume 1.75 x Secant Modulus)		fy = 60,000 psi	Initial yield stress
f΄c = 5,000 psi	Compressive strength of concrete (SIGMAC)		Ds = 0.0007339 lb-sec2/in4	Density
εc = 0.002	Compressive strain of concrete at SIGMAC
f΄uc = 4,250 psi	Ultimate compressive strength of concrete (SIGMAU, assumed @ 85% f΄c)
εuc = 0.003	Ultimate compressive strain of concrete at SIGMAU
fr = 5√ f΄c = 353.6 psi	Uniaxial cut-off tensile strength of concrete
νc = 0.20	Poisson’s Ratio
wtc = 145 lbs/ft3	Weight
Dc = 0.00021716366 lb-sec2/in4	Density
Φp = 0.55	Strength reduction factor for plain concrete

Array
Array
Array
Array
within the body of the panel

Array
Array

Array
Array
Array
Array
Array
within the body of the panelANIMATIONS
Reinforcement Considerations
Array
## CONCLUSIONS AND RECOMMENDATIONS
Conclusions
Recommendations
ACKNOWLEDGMENT
## See Also
Place text here.
## References
Concrete International
Addresshttp://www.umanitoba.ca/cast_building/resources.html
Concrete International
ADINAAvailable
ADINA – Theory and Modeling Guide
Test Method for Tensile Properties of Geotextiles by the Wide Width Strip Method
Amoco 2006 Stress Strain
Geosynthetics International
Amoco 2006 Relaxation Results
Addresshttp://www.terram.co.uk
## External Links
The Centre for Architectural Structures and Technology (C.A.S.T.)
Fabric-Formed Concrete